## Slide 1
Laminate R-1566S
Prepreg R-1551S
Data Sheet
June 2025 No.250606
High heat resistance halogen-free
multi-layer circuit board materials
Notes: Dk；1桁表示
樹脂量；71％以上，61％，62％の8G,10GHz修正

## Slide 2
Sample thickness ; 32 mil ( 0.8 ㎜ )
Specification / Laminate R-1566S
Property |  |  | Units | Test Method | Condition | Typical Value
THERMAL | Glass Transition Temp ( Tg ) |  | ˚C | DSC | As received | 175
 |  |  |  | TMA | As received | 170
 |  |  |  | DMA | As received | 195
 | Thermal Decomposition Temp ( Td ) |  | ℃ | TGA | As received | 355
 | Time to Delam ( T288 ) | Without Cu | Min | IPC TM-650 2.4.24.1 | As received | > 120
 |  | With Cu | Min | IPC TM-650 2.4.24.1 | As received | 10
 | CTE : α1 | X - axis | ppm / C | IPC TM-650 2.4.24 | < Tg | 11 – 13
 |  | Y ‐ axis | ppm / C | IPC TM-650 2.4.24 | < Tg | 13 – 15
 |  | Z - axis | ppm / C | IPC TM-650 2.4.24 | < Tg | 40
 | CTE : α2 | Z - axis | ppm / C | IPC TM-650 2.4.24 | > Tg | 180
ELECTRICAL | Volume Resistivity |  | MΩ - cm | IPC TM-650 2.5.17.1 | C-96/35/90 | 1 x 10 9
 | Surface Resistivity |  | MΩ | IPC TM-650 2.5.17.1 | C-96/35/90 | 1 x 10 8
 | Dielectric Constant ( Dk ) | @ 1MHz | - | IPC TM-650 2.5.5.9 | C-24/23/50 | 5.0
 |  | @ 1GHz | - | IPC TM-650 2.5.5.9 | C-24/23/50 | 4.7
 | Dissipation Factor ( Df ) | @ 1MHz | - | IPC TM-650 2.5.5.9 | C-24/23/50 | 0.011
 |  | @ 1GHz | - | IPC TM-650 2.5.5.9 | C-24/23/50 | 0.011
PHYSICAL | Water Absorption |  | % | IPC TM-650 2.6.2.1 | D-24/23 | 0.18
 | Peel Strength | 1oz | kN / m | IPC TM-650 2.4.8 | As Received | 1.6
 | Flammability |  | - | UL 94V | C-48/23/50 | 94V-0 †1
†1 The value represents Panasonic internal test results based on the UL94 test method for flammability and is NOT intended
to indicate that the product is UL certified. If UL certification is required, use R-156AS or R-156YS for the UL recognized grades.
* Our Halogen-free materials are based on JPCA-ES-01-2003 standard and others.
Notes: 2019.2.28 Tg-DMA 190℃ → 195℃

## Slide 3
Specification / Laminate R-1566S

## Slide 4
Specification / Prepreg R-1551S